## Slide 2
RECIPROCAL LATTICE
The orientation of a plane is defined by the direction of a normal to the plane:

## Slide 3
RECIPROCAL LATTICE
dhkl vectors in the direct space
d*hkl vectors in the reciprocal space
[Å]
[1/Å]

## Slide 4
RECIPROCAL LATTICE
The reciprocal lattice is periodic.
Therefore, we should be able to define the reciprocal unit cell:
(a*, b*, c*)
such that any vector in the lattice can be described as
d*hkl = ha* + kb* + lc*
Now let’s see how the reciprocal lattice
is related to the diffraction pattern

## Slide 5
Why Use The Reciprocal Space?
Think about the Bragg law:
What do we measure experimentally?
Angles at which diffraction
maxima are observed

## Slide 6
x
r1
r2

Why Use The Reciprocal Space?
The experimental measurement is directly related to d*hkl OR
The detector is scanning for the reciprocal lattice points d*hkl

## Slide 7
Why Use The Reciprocal Space?
Diffraction from a single Xtal
A diffraction pattern is not a direct representation of the crystal lattice
The diffraction pattern is a representation of the reciprocal lattice
In order to find the reciprocal lattice,
the diffraction pattern can be indexed

## Slide 8
INDEXING PROCEDURE
To index a diffraction pattern means:
to find such a basis (a*,b*,c*) that
all the diffraction spots (or lines)
can be described (indexed) as
d*hkl = ha* + kb* + lc*
with only integer (hkl) values allowed.
All we need to do is to find the value of d* for each spot and then let software find the unit cell.
Basically, we deal with a system of linear equations.
The more reflections we have,
the more reliably the unit cell will be determined.

## Slide 9
THE RECIPROCAL UNIT CELL
The reciprocal UC is related to the direct UC:
By definition
a*·a = 1 b*·a = 0 c*·a = 0
a*·b = 0 b*·b = 1 c*·b = 0
a*·c = 0 b*·c = 0 c*·c = 1
which means that
a*  (bc) b*  (ac) c*  (ab)
If we can index the diffraction pattern
and find the reciprocal UC,
then we will be able to find the direct UC.
c
b
a*


## Slide 10: Draw the reciprocal unit cell (b axis is  to the plane of the paper)
THE RECIPROCAL UNIT CELL

## Slide 11
Families of planes
(100) (200) (300)
diffraction crystal planes -
(100), (200), …
(100)
(200)
Lattice plane directions-(100)

## Slide 12
3. Reciprocal lattice
A reciprocal lattice point corresponds to a diffraction (lattice) plane of its original lattice.
A reciprocal vector r* is perpendicular to a lattice plane with the indices (hkl).